## Slide 1: Towards Super-Resolution Structural Characterization of Biomacromolecules in Solution
Jiahui Chen
Postdoc Appointee
Structural Science group, X-ray Science Division
Argonne National Laboratory
May 13, 2022

## Slide 2: outline
Introduction
  Understand Structure of Biomacromolecules
SAXS, Ultra-Wide Angles Scattering Experiments, and PDF analysis
  Benchmark Sample: Mo132, Cyclodextrin
  Application: Chain Conformation, Counterion Condensation
Summary and Looking Forward

## Slide 3
Introduction

## Slide 4: understand the structure and function of biomacromolecules
Understanding of the structures of biomacromolecule is essential for structure-function relationship knowledge and rational drug design.
Binding of PF-00835231 (left, initial inhibitor candidate) and PF-07321332 (middle, one of component in Pfizer’s PAXLOVID™) with SARS-COV-2 main protease dimer (right)
https://en.wikipedia.org/wiki/Coronavirus_spike_protein
Science.374 (2021): 1586-1593.

## Slide 5: High resolution characterization: X-ray Crystallography and Cryo-EM
https://upload.wikimedia.org/wikipedia/commons/7/73/X_ray_diffraction.png
Methods in enzymology 579 (2016): 51-86.
Require significant amount of effort to prepare samples.

## Slide 6: Small angle X-ray Scattering (SAXS)
A common instrumental setup of a small angle scattering experiment.
Fourier transformation
Pair Density Distribution Function (PDDF) analysis
Credit:
Nat. Rev. Methods Primers 1, (2021): 70
Credit:
Biophys J. 110 (2016):2185
Kratky plot

## Slide 7: Small angle X-ray Scattering (SAXS)
Information that can be extracted from SAXS data.
Credit: Nature Reviews Methods Primers 1, (2021): 70
A reconstructed 3D structure from SAXS data
I(0):
Molecular weight and concentration
q

## Slide 8: Small angle X-ray Scattering (SAXS)
Advantages:
Require little to no sample preparation.
Rapid data collection.
In vitro measurements at physiological condition is possible.
Disadvantages:
Low resolution: 1~2 nm. Continuum assumption on solvent and solute.
Radiation damage can be significant for biomacromolecules. The damaged sample frequently adheres to capillary cell and affect all following experiment
Usually require previous knowledge to analyze the data (high resolution structure from MD, Cryo-EM, NMR, or crystallography)

## Slide 9: From SAXS to WAXS
Most of SAXS experiments on biomacromolecular solutions only take qmax < 0.3 Å-1 , corresponding to a resolution ~ 2 nm.
Scattering profile will contain more information with higher qmax.

## Slide 10
SAXS and Ultra-Wide Angles Scattering Experiments for Atomic PDF analysis

## Slide 11: Information in the extended q-range data
SAXS
PXRD
PDF

## Slide 12: Combination of saxs and waxs instruments
15 ID-D, SAXS
q-range: 0.04~1.8 Å-1
@ 20 Kev
NSF’s ChemMatCARS
11 ID-B, WAXS
q-range: 1.5 ~ 23 Å-1
@ 58 Kev
Advanced Photon Source
12 ID-B, SEC-SAXS
q-range: 0.001~2.5 Å-1
@ 12 Kev

## Slide 13: Benchmark sample-Mo132
2.9 nm
[Mo132O372(H2O)72(CH3CO2)30]
High-Z Elements,
Rigid, Well-Defined Structure.
Size comparable to a protein
I-q(WAXS)

## Slide 14: Benchmark sample-Mo132
Merge with SAXS
Fourier Transform
I-q(SAXS+WAXS)
PDF Profile

## Slide 15
Peak position at low-r: apparent bond length
Features at high-r: Particle size and shape
2.9 nm

## Slide 16: Benchmark on PDF analysis of Biomacromolecules
Credit: Food. Bioproc. Tech. 12, (7) (2019): 1157-1173.
12 Å
Crystalline structure
Low-Z material, Well-defined and Rigid Conformation
Cyclodextrins are widely used in small molecule drug formulation to increase solubility and change metabolism.
However, the inclusive complex usually do not crystallize, which makes it difficult to characterize the structure by conventional crystallography methods.
Inclusion complexes of a βCD derivative with Remdesivir
Credit: J Pharm Biomed Anal. 209, (2022);114482.

## Slide 17: Scattering data
I-q(WAXS)
I-q(SAXS+WAXS)

## Slide 18: Atomic PDF analysis
Macrocycle Conformation
Intra-glucosidic ring covalent bonding
Fourier Transform
I-q(SAXS+WAXS)
PDF Profile

## Slide 19
structure determination and refinement

## Slide 20: Chain conformation
 | Center / Å | Area | FWHM | Bond
1 | 1.04 | 0.604 | 0.174 | C-H/O-H
2 | 1.44 | 2.620 | 0.269 | C-C/C-O
3 | 2.41 | 1.322 | 0.214 | Two Bonds
4 | 2.82 | 0.551 | 0.224 | Hydrogen Bond/Para-Positions in the Glucosidic Ring
5 | 3.69 | 0.429 | 0.249 | O2-C4, O3-C5…..
6 | 4.22 | 0.345 | 0.207 | O2-C5, O3-O5…..
Initial structure
Refined structure

## Slide 21: Counterion association

## Slide 22: Counterion association and Chain conformation
Initial structure, determined at low concentration and low ionic strength
Refinement result
50
125 mg/ml Heparin sodium salt
Sodium Counterion Association

## Slide 23: Improved resolution compared with SAXS PDF profile
Particle size and shape
Short range correlation
Information about short range correlation is missing in the SAXS
WAXS+SAXS PDF profile
SAXS only PDF profile (< 1 Å-1)

## Slide 24: Looking forward to protein

## Slide 25: Looking forward to protein

## Slide 26: Summary
Combined SAXS and WAXS beamlines to achieve wide q-range coverage on biomacromolecule solution X-ray scattering measurement.
Atomic PDF analysis is a promising method to make use of WAXS data to determine and refine structures for biomacromolecules in pharmaceutically relevant environment.

## Slide 27: acknowledgement
Dr. Olaf J. Borkiewicz
Dr. Uta Ruett
Dr. Xiaobing Zuo
Dr. Fan Zhang
Dr. Igor Levin
Dr. Alexander Grishaev
Dr. Mrinal K. Bera

## Slide 29: Alpha CD
Simulated | Observed
q / Å-1 | q / Å-1
0.79 | 0.83
1.42 | 1.52
1.97 | 1.98
2.54 | 2.58
3.38 | 3.43
5.26 | 5.22
7.9 | 7.9
9.0 | 9.0
11.1 | 11.0
13.7 | 13.7
Simulated (crysol) and Experimental I-q Data

## Slide 30: Alpha CD
G(r) Extracted from Simulated and Experimental Data
The simulated one from a structure without considering atom thermal motion, resulting in sharper peaks

## Slide 31: Atomic Structure Function
Structure Function
(different from the structure factor used in SAXS community)
I(q) normalized by atomic form factor
Various corrections: q Space Resampling, Data Smoothing, Linear Interpolate q to 0….

## Slide 32: G(r) profile
Inter-glucosidic ring conformation
Hydration layer
Intra-glucosidic ring covalent bonding
Fourier transformation
Optional: Dump q[S(q)-1] to suppress high-frequency noise

## Slide 33: Why do need both SAXS and WAXS data?
WAXS:
qmax determines the r-space resolution:
, for a qmax 20 Å-1, 0.15 Å-1
Also, qmax determines amplitude of termination artifacts:
Ideally, S(q) converge to 1 at qmax. If not, the sudden step down of S(q) at qmax will give a sinc-function like ripples convoluted with G(r).

## Slide 34: Effect of qmax on the extraction of G(r)
Credit:
J. Chem. Phys. 138, 074506 (2013)
The effect of qmax on peak positions has been observed on pair distribution function analysis of water as well.
qmin = 10 to 27 Å-1

## Slide 35: Effect of qmax on the extraction of G(r)
PDF profile extracted from experimental scattering data of 50 mg/ml ACD solution.

## Slide 36: Effect of qmin on the extraction of G(r)
SAXS:
Fourier transformation of SAXS part gives the baseline of the PDF profile at high-r.
PDF profile extracted from experimental scattering data of 50 mg/ml ACD solution.

## Slide 37: Do we need to extend qmin?
When q ~ 0 (small angle), sin(qr) ~ qr,
S(q3) ~ constant ~ I0/<b>2 (Guinier approximation):
For a typical protein with diameter ~ 2 nm:
S(0) = ~ 100, ~ 0.08 Å-3, minimum peak height in G(r) ~ 0.1 Å-2
when qmin = 0.05 Å-1 ~ 0.001 Å-2
should be much smaller than G(r) at any r.

## Slide 38: Instrument resolution
Where is the q resolution function, is the instrument resolution
As for scattering from single particle/amorphous material, there is no sharp Bragg peaks. Therefore, intensity is a continuous function and effect of q resolution is minimum.

## Slide 39: instrument resolution
Where is the q resolution function, is the instrument resolution
As for scattering from single particle/amorphous material, there is no sharp Bragg peaks.
Therefore, intensity is a continuous function,
, and effect of q resolution is minimum.

## Slide 40: PDF for single particle scattering
Given that the molecules are random and isotropically oriented in solution:
Pair Distribution Function
Histogram of Atomic Distance
For a system of infinity size, like “bulk” crystal, amorphous materials, and liquids, , and is well-defined.
For a single particle of limited size, ideally when r is beyond the dimension of the particle, and is ambiguous.
: Number density of atoms

## Slide 41: PDF for single particle scattering
[-1]
Reduced Pair Distribution Function
Derivation of averaged atomic number density
For a single particle of limited size:
At low-r, , but is ambiguous.
when r is beyond the dimension of the single particle?
For a system of infinity size:
At low-r, , as = 0 when r is below the minimum distance between atoms.
At high-r, , as = 1.

## Slide 42: PDF for single particle scattering
Debye scattering equation:
The distance between atoms i and j
Atomic scattering factor
For a single particle in solution, the scattering can be separated as
the scattering from particle.
the scattering from r beyond the dimension of the particle size, which is the cross-correlation from the particle and solvent.
the scattering from solvent, which has been subtracted during the data reduction.

## Slide 43
Does not converge!!
Normalized scattering intensity from the particle minus excluded solvents
Laue monotonic scattering, to normalize I(q) to at high q

## Slide 44
Assuming inter-particle correlation and the correlation between the medium (solvents) and the particle is negligible.
The scattering from solvents can be totally subtracted, and no intensity contribution from the cross-term between solvents and particle.
Then, the space beyond the dimension of the particle can be treated as vacuum.

## Slide 45
The space beyond the dimension of the particle, vacuum.
[-1]=
Still does not converge!!

## Slide 46
The space beyond the dimension of the particle is vacuum.
= 0
The second term becomes 0
Normalized scattering intensity from the particle minus excluded solvents

## Slide 47: Alpha CD @ 12-ID-B

## Slide 48: Alpha CD
G(r) Extracted from Simulated and Experimental I(q) Data
The simulated one from a structure without Debye-Waller factor and hydration layer
Sharper peaks, lower peak area at 2.8 Å (Oxygen-Oxygen distance in a hydrogen bond), and no features beyond 12 Å (hydration layer).

## Slide 49: Heparin structure
PDB entry 3IRJ, structure determined by SAXS, 0.5 mg/ml
Heavily charged, semi-rigid polysaccharide chain

## Slide 50: Heparin scattering data
125 mg/ml Heparin sodium salt aqueous solution
Mw ~ 20KDa

## Slide 51: PDDF analysis and Kratky plot
Kratky Plot
PDDF
The polysaccharide chain is most likely folded.

## Slide 52
The G(r) profiles also shows huge difference between experimental extracted profile and the profile calculated from semi-rigid chain model.
Initial Model
50
G(r) profiles

## Slide 53: Heparin structural refinement
Define each saccharide ring as a rigid body and allow torsion angle to change between the rings.
Simulated annealing: Monte Carlo simulation on torsion angles until the G(r) profile matches

## Slide 54
0.087 atoms/Å3
1156 atoms (with crystalline water): 13287 Å3
1012 atoms (without crystalline water): 11632 Å3
Excluded volume from crysol: 12520 Å3

## Slide 55
0.087 atoms/Å3
1156 atoms (with crystalline water): 13287 Å3
1012 atoms (without crystalline water): 11632 Å3
Excluded volume from crysol: 12520 Å3
0.075 atoms/Å3
1156 atoms (with crystalline water): 15413 Å3
1012 atoms (without crystalline water): 13493 Å3
Excluded volume from crysol: 12520 Å3
0.088 atoms/Å3
1156 atoms (with crystalline water): 13136 Å3
1012 atoms (without crystalline water): 11500 Å3
Excluded volume from crysol: 12520 Å3

## Slide 56: What is the PDF?
1.42 Å
1.42 Å
1.42 Å
2.47 Å
2.47 Å
2.83 Å
2.83 Å
1.42 Å
2.47 Å
3.76 Å
2.83 Å
1.42 Å
2.47 Å
3.76 Å
2.83 Å
1.42 Å
2.47 Å
3.76 Å
4.27 Å
4.27 Å
Probability of finding a pair of atoms at various distances

## Slide 57: The Pair Distribution Function, G(r)
- a weighted histogram of ALL atom-atom distances
Providing valuable structural insight for:
Nanoscale materials
Disordered materials
Liquids, gases
Vacancies, impurities, interstitial atoms

## Slide 58: The Pair Distribution Function, G(r)
Peak Position Atomic distances
A
B
C
C
A
B
Direct extraction of parameters from PDF (peak fitting)
Peak Position
Peak Area
Peak Width
Peak rmax
Atomic distances
Coordination number
Disorder
Particle size, coherence

## Slide 59: The Pair Distribution Function, G(r)
Peak Area Number of pairs weighted by scattering power
i.e. coordination number &/or concentration
C
A
B
12 neighbors
12 neighbors
6 neighbors
A
B
C
Peak Position
Peak Area
Peak Width
Peak rmax
Atomic distances
Coordination number
Disorder
Particle size, coherence

## Slide 60: The Pair Distribution Function, G(r)
Peak Width Disorder
C
A
B
C
Peak Position
Peak Area
Peak Width
Peak rmax
Atomic distances
Coordination number
Disorder
Particle size, coherence

## Slide 61: The Pair Distribution Function, G(r)
Peak rmax Particle size, coherence
rmax
Peak Position
Peak Area
Peak Width
Peak rmax
Atomic distances
Coordination number
Disorder
Particle size, coherence

## Slide 62: PDF vs Coherence
Crystalline well ordered
Crystalline disordered
Nanomaterial
Amorphous

## Slide 63: For more information
“Underneath the Bragg Peaks” 2nd Ed. (2012)
Takeshi Egami & Simon J.L. Billinge
Toby, B.H. and T. Egami, (1992) Accuracy of Pair Distribution Function-Analysis Applied to Crystalline and Noncrystalline Materials. Acta Cryst. A, 48: p. 336-346.

## Slide 64: Data Reduction Process
6. Data Analysis / Modeling
2. I(Q) Integration
+ background correction
3. Calculate S(Q)
4. Calculate F(Q)
5. Fourier transform to get G(r)
1. Collect 3D data

## Slide 65: Local coordination geometry: EXAFS vs. PDF
EXAFS (r < 6 Å)
Atomic scale resolution over a few coordination shells
Bond lengths available after correcting for phase shift
Intrinsically element specific
Elements must have edge at appropriate energy
PDF (r >> 6 Å)
Atomic scale resolution over many coordination shells, > 100Å
Bond lengths correspond directly to peak position
Not element specific. Sees all (but we can recover chemical specificity)
r / Angstrom
Pt foil Pt L3-edge
Vaarkamp et al. PRB 1994 7872
Data in ~0.03 sec